SportMaster Sport Surfaces
August 2009
PO Box 2277
2520 South Campbell Street

Sandusky, Ohio 44870
Toll Free
800-326-1994
Fax
877-825-9226
Website
www.sportmaster.net
E-mail
info@sportmaster.net
Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice, Fifth Edition.
This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers are from MasterFormat 1995 Edition, with section numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION 02790 (32 18 23.43)

CONCRETE INLINE SKATE AND HOCKEY SURFACE COLOR COATING SYSTEM
Specifier Notes:  This section covers SportMaster Sport Surfaces “SportMaster” concrete inline skate and hockey surface color coating system.  Consult SportMaster Sport Surfaces for assistance in editing this section for the specific application.

PART 1
GENERAL

1.1
SECTION INCLUDES

A.
Concrete inline skate and hockey surface color coating system.
1.2
RELATED REQUIREMENTS
Specifier Notes:  Edit the following list of related sections as required.  Delete related sections not required.  List other sections with work directly related to this section.

A.
Section 03300 (03 30 00) – Cast-in-Place Concrete.
B.
Section 03400 (03 40 00) – Precast Concrete.

1.3
REFERENCE STANDARDS
Specifier Notes:  List reference standards mentioned in this section, complete with designations and titles.  Delete reference standards not included in this edited section.  This article does not require compliance with reference standards, but is merely a listing of those used.
A.
American Sports Builders Association (ASBA).

B.
USA Hockey InLine (USAHIL) official rules.
1.4
SUBMITTALS

Specifier Notes:  Edit submittal requirements as required.  Delete submittals not required.

A.
Comply with Section 01330 (01 33 00) – Submittal Procedures.

B.
Product Data:  Submit manufacturer’s product data, including surface and crack preparation and application instructions.

Specifier Notes:  Delete samples if not required.

C.
Samples:  Submit manufacturer’s color samples of color coating.

Specifier Notes:  Submit independent test results for solar reflectance index to qualify for LEED credits.

D.
Test Reports:  Submit independent test results for solar reflectance index.

E.
Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

F.
Manufacturer’s Project References:  Submit manufacturer’s list of successfully completed concrete inline skate and hockey surface color coating system projects, including project name, location, and date of application.
G.
Applicator’s Project References:  Submit applicator’s list of successfully completed concrete inline skate and hockey surface color coating system projects, including project name, location, type and quantity of color coating system applied, and date of application.
H.
Warranty Documentation:  Submit manufacturer’s standard warranty.
1.5
QUALITY ASSURANCE

A.
Manufacturer’s Qualifications:

1.
Manufacturer regularly engaged, for past 5 years, in manufacture of concrete inline skate and hockey surface color coating systems of similar type to that specified.
2.
United States owned company.

3.
Member:  ASBA.
B.
Applicator's Qualifications:

1.
Applicator regularly engaged, for past 3 years, in application of inline skate and hockey surface color coating systems of similar type to that specified.
2.
Employ persons trained for application of inline skate and hockey surface color coating systems.
1.6
DELIVERY, STORAGE, AND HANDLING
A.
Delivery and Acceptance Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.
Storage and Handling Requirements:
1.
Store and handle materials in accordance with manufacturer’s instructions.

2.
Keep materials in manufacturer’s original, unopened containers and packaging until application.
3.
Store materials in clean, dry area indoors.

4.
Store materials out of direct sunlight.

5.
Keep materials from freezing.

6.
Protect materials during storage, handling, and application to prevent contamination or damage.

7.
Close containers when not in use.
1.7
AMBIENT CONDITIONS
A.
Do not apply concrete inline skate and hockey surface color coating system when air or surface temperatures are below 50 degrees F during application or within 24 hours after application.
B.
Do not apply concrete inline skate and hockey surface color coating system when rain is expected during application or within 24 hours after application.

PART 2
PRODUCTS

2.1
MANUFACTURER

A.
SportMaster Sport Surfaces, PO Box 2277, 2520 South Campbell Street, Sandusky, Ohio 44870.  Toll Free 800-326-1994.  Fax 877-825-9226.  Website www.sportmaster.net.  E-mail info@sportmaster.net.

2.2
MATERIALS
A.
Concrete Inline Skate and Hockey Surface Color Coating System:  SkateMaster Coating System.

B.
Crack Filler:  SportMaster “Acrylic Crack Patch”.
1.
100 percent acrylic emulsion trowel-grade crack filler.

2.
Fills cracks in concrete pavement up to 1 inch wide.

3.
Chemical Characteristics, by Weight, Minimum:

a.
Acrylic Emulsion:  10.0 percent.

b.
Hiding Pigment:  0.2 percent.

c.
Mineral Inert Fillers:  78.0 percent.

d.
Film Formers, Additives:  1.8 percent.

e.
Water:  8.5 percent.
4.
Weight per Gallon at 77 Degrees F:  15.2 lbs., plus or minus 1.0 lbs.

5.
Non-Volatile Material:  80 percent, plus or minus 5 percent.
Specifier Notes:  Specify color of crack filler.

6.
Color:  [Green]  [Neutral]  [Red].
C.
Patch Binder:  SportMaster “Acrylic Patch Binder”.
1.
100 percent acrylic emulsion liquid binder.

2.
Mix on-site with sand and cement.

3.
Levels and repairs low spots and depressions up to 3/4 inch deep in concrete pavement.

4.
Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

D.
Adhesion Promoter:  SportMaster “Acrylic Adhesion Promoter”.

1.
Acrylic emulsion primer.

2.
Primes concrete surface and promotes adhesion of inline skate and hockey system materials.

3.
Weight per Gallon at 77 Degrees F:  8.7 lbs., plus or minus 0.5 lbs.

E.
Filler Course:  SportMaster “Neutral Acrylic Resurfacer”.

1.
100 percent acrylic emulsion resurfacer.

2.
Mix on-site with silica sand (14lbs of sand per gallon – 70 mesh or finer).

3.
Apply to adhesion promoter or previously colored acrylic surfaces in preparation of SkateMaster color coating system.

4.
Chemical Characteristics, by Weight, Minimum:

a.
Acrylic Emulsion:  44.0 percent.

b.
Hiding Pigment:  2.0 percent.

c.
Mineral Inert Fillers:  5.0 percent.

d.
Film Formers, Additives:  0.2 percent.

e.
Water:  45.0 percent.
5.
Weight per Gallon at 77 Degrees F:  8.5 lbs., plus or minus 0.5 lbs.

6.
Non-Volatile Material:  27.5 percent, plus or minus 5.0 percent.
7.
Color:  Neutral – Follow manufacturers’ specifications for tinting Filler Course.
F.
Skate Surface:  SportMaster “SkateMaster Coating System”.

1.
100 percent acrylic emulsion coating.

2.
Product ready to mix and apply.  Do not dilute or add sand.

3.
Color coats Inline skate and hockey recreational areas.

4.
Weight per Gallon at 77 Degrees F:  9.2 lbs., plus or minus 0.5 lbs.

Specifier Notes:  Specify color of color coating.  The following colors can contribute to LEED credits for SS Credit 7.1: Heat Island Effect – Non-Roof:  Dove Gray, Ice Blue, Light Green, Red, and Sandstone.

5.
Color:  [Beige]  [Blue]  [Brown]  [Dark Green]  [Dove Gray]  [Forest Green]  [Gray]  [Ice Blue]  [Light Blue]  [Light Green]  [Maroon]  [Red]  [Sandstone]  [Tournament Purple].

G.
Line Markings Primer:  SportMaster “Stripe-Rite”.
1.
100 percent acrylic emulsion primer, clear drying.

2.
Primes line markings and prevents bleed-under for sharp lines.
3.
Chemical Characteristics, by Weight, Nominal:

a.
Acrylic Emulsion:  38.0 percent.

b.
Hiding Pigment:  0.0 percent.

c.
Mineral Inert Fillers:  7.0 percent.

d.
Film Formers, Additives:  1.5 percent.

e.
Water:  50.0 percent.
4.
Weight per Gallon at 77 Degrees F:  8.9 lbs., plus or minus 0.5 lbs.

5.
Non-Volatile Material:  29 percent, plus or minus 5 percent.
H.
Line Paint:  SportMaster “Textured Line Paint”.
1.
Pigmented, 100 percent acrylic emulsion line paint.

2.
Line marking on concrete inline skate and hockey areas.
3.
Chemical Characteristics, by Weight, Nominal:

a.
Acrylic Emulsion:  25.89 percent.

b.
Pigment:  14.90 percent.

c.
Mineral Inert Fillers:  13.12 percent.

d.
Additives:  4.73 percent.

e.
Water:  41.36 percent.
4.
Weight per Gallon at 77 Degrees F:  10.65 lbs., plus or minus 0.75 lbs.

5.
Non-Volatile Material:  45.17 percent, plus or minus 5 percent.
Specifier Notes:  Specify color of line paint.

6.
Color:  [Blue]  [Red]  [White]  [Yellow].

PART 3
EXECUTION

3.1
EXAMINATION

A.
Examine concrete inline skate and hockey surfaces to receive skate surfacing system.
B.
Verify:

1.
Suitable vapor barrier beneath concrete slab.

2.
Perimeter drainage to prevent moisture accumulation beneath concrete surface.


3.      No curing compounds have been applied to surface.
4.
Concrete inline skate and hockey courts meet ASBA requirements.
C.
Notify Architect of conditions that would adversely affect application or subsequent use.
D.
Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2
SURFACE PREPARATION

A.
Protection of In-Place Conditions:  Protect adjacent surfaces and landscaping from contact with concrete inline skate and hockey surface color coating system.
B.
Prepare surfaces in accordance with manufacturer’s instructions.

C.
New Concrete:

1.
Cure new concrete surfaces a minimum of 28 days before application of concrete inline skate and hockey surface color coating system.
2.
Provide medium broom finish or similar roughened texture.

3.
Do not steel trowel finish.


4.      Acid etch with phosphoric or muriatic acid and rinse thoroughly prior to application of color 


         coating system.
D.
Existing Concrete:

1.
Sandblast, shotblast, or scarify smooth concrete surfaces to roughened texture similar to medium broom finish.
2.
If existing concrete is uncoated, acid etch with phosphoric or muriatic acid and rinse thoroughly prior to application of color coating system.
E.
Remove dirt, dust, debris, oil, grease, sealers, curing compounds, vegetation, loose coatings, loose materials, and other surface contaminants which could adversely affect application of concrete inline skate and hockey surface color coating system.  Pressure wash entire surface.
F.
Repair cracks, depressions, and surface defects in accordance with manufacturer’s instructions before application of skate surface.
G.
Repair spalled areas and level depressions 1/8 inch and deeper with patch binder in accordance with manufacturer’s instructions.
H.
Apply adhesion promoter over entire concrete surface in accordance with manufacturer’s instructions.
I.
Apply 1 coat of filler course to provide smooth underlayment for application of skate surface.

J.
Ensure surface repairs are flush and smooth to adjoining surfaces.
3.3
APPLICATION

A.
Apply concrete inline skate and hockey surface color coating system in accordance with manufacturer’s instructions at locations indicated on the Drawings.

B.
Mix materials in accordance with manufacturer’s instructions.

C.
Apply Filler Course and Skate Surface with a 50-60 durometer, soft rubber squeegee.

D.
Filler Course:

1.      Apply 1 coat on new concrete or existing acrylic surfaces with minimal repairs.
2.      Apply 2 coats on existing acrylic surfaces with extensive cracks or low spot repair.
E.
Skate Surface:  Apply a minimum of 2 coats of Skate Surface to prepared surfaces in accordance with manufacturer’s instructions.

F.
Allow material drying times in accordance with manufacturer’s instructions before applying other materials or opening completed surface to foot traffic.
3.4
LINE MARKINGS

A.
Lay out inline skate and hockey court line markings in accordance with USA Hockey InLine (USAHIL) official rules.

B.
Apply line markings primer, after masking tape has been laid, to seal voids between masking tape and court surface to prevent bleed-under when line paint is applied.

C.
Apply a minimum of 1 coat of line paint in accordance with manufacturer’s instructions.
3.5
PROTECTION

A.
Allow a minimum of 24 hours curing time before opening inline skate and hockey courts for play.

B.
Protect applied concrete inline skate and hockey surface color coating system to ensure that, except for normal weathering, coating system will be without damage or deterioration at time of Substantial Completion.
END OF SECTION
SportMaster Concrete Inline Skate and Hockey
Surface Color Coating System
02790 (32 18 23.43) - 7

