SportMaster Sport Surfaces
September 2010
PO Box 2277

2520 South Campbell Street

Sandusky, Ohio 44870

Toll Free
800-326-1994

Fax
877-825-9226

Website
www.sportmaster.net
E-mail
info@sportmaster.net
Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice, Fifth Edition.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers are from MasterFormat 1995 Edition, with section numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION 02790 (32 18 23.53)

CONCRETE TENNIS COURT CUSHIONED SURFACE COLOR COATING SYSTEM

Specifier Notes:  This section covers SportMaster Sport Surfaces “SportMaster” concrete tennis court cushioned surface color coating system.  Consult SportMaster Sport Surfaces for assistance in editing this section for the specific application.

PART 1
GENERAL

1.1
SECTION INCLUDES

A.
Concrete tennis court cushioned surface color coating system.

1.2
RELATED REQUIREMENTS

Specifier Notes:  Edit the following list of related sections as required.  Delete related sections not required.  List other sections with work directly related to this section.

A.
Section 03300 (03 30 00) – Cast-in-Place Concrete.

B.
Section 03400 (03 40 00) – Precast Concrete.

1.3
REFERENCE STANDARDS

Specifier Notes:  List reference standards mentioned in this section, complete with designations and titles.  Delete reference standards not included in this edited section.  This article does not require compliance with reference standards, but is merely a listing of those used.

A.
American Sports Builders Association (ASBA).

B.
United States Tennis Association (USTA) Rules of Tennis.

1.4
SUBMITTALS

Specifier Notes:  Edit submittal requirements as required.  Delete submittals not required.

A.
Comply with Section 01330 (01 33 00) – Submittal Procedures.

B.
Product Data:  Submit manufacturer’s product data, including surface and crack preparation and application instructions.

Specifier Notes:  Delete samples if not required.

C.
Samples:  Submit manufacturer’s color samples of color coating.

Specifier Notes:  Submit independent test results for solar reflectance index to qualify for LEED credits.

D.
Test Reports:  Submit independent test results for solar reflectance index.

E.
Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

F.
Manufacturer’s Project References:  Submit manufacturer’s list of successfully completed concrete tennis court cushioned surface color coating system projects, including project name, location, and date of application.

G.
Applicator’s Project References:  Submit applicator’s list of successfully completed concrete tennis court cushioned surface color coating system projects, including project name, location, type and quantity of color coating system applied, and date of application.

H.
Warranty Documentation:  Submit manufacturer’s standard warranty.

1.5
QUALITY ASSURANCE

A.
Manufacturer’s Qualifications:

1.
Manufacturer regularly engaged, for past 5 years, in manufacture of concrete tennis court cushioned surface color coating systems of similar type to that specified.

2.
United States owned company.

3.
Member:  ASBA.  

B.
Applicator's Qualifications:

1.
Applicator regularly engaged, for past 3 years, in application of concrete tennis court cushioned surface color coating systems of similar type to that specified.

2.
Employ persons trained for application of concrete tennis court cushioned surface color coating systems.

1.6
DELIVERY, STORAGE, AND HANDLING

A.
Delivery and Acceptance Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.
Storage and Handling Requirements:

1.
Store and handle materials in accordance with manufacturer’s instructions.

2.
Keep materials in manufacturer’s original, unopened containers and packaging until application.

3.
Store materials in clean, dry area indoors.

4.
Store materials out of direct sunlight.

5.
Keep materials from freezing.

6.
Protect materials during storage, handling, and application to prevent contamination or damage.

7.
Close containers when not in use.

1.7
AMBIENT CONDITIONS

A.
Do not apply concrete tennis court cushioned surface color coating system when air or surface temperatures are below 50 degrees F during application or within 24 hours after application.

B.
Do not apply concrete tennis court cushioned surface color coating system when rain is expected during application or within 24 hours after application.

PART 2
PRODUCTS

2.1
MANUFACTURER

A.
SportMaster Sport Surfaces, PO Box 2277, 2520 South Campbell Street, Sandusky, Ohio 44870.  Toll Free 800-326-1994.  Fax 877-825-9226.  Website www.sportmaster.net.  E-mail info@sportmaster.net.

2.2
MATERIALS

A.
Concrete Tennis Court Cushioned Surface Color Coating System:  SportMaster ProCushion System.

B.
Crack Sealant:  SportMaster “Crack Magic”.

1.
100 percent acrylic emulsion elastomeric crack sealant.

2.
Seals cracks up to 1/2 inch wide in concrete pavement.

3.
Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

4.
Non-Volatile Material:  61 percent, plus or minus 5 percent.

C.
Crack Filler:  SportMaster “Acrylic Crack Patch”.

1.
100 percent acrylic emulsion trowel-grade crack filler.

2.
Fills cracks in concrete pavement up to 1 inch wide.

3.
Chemical Characteristics, by Weight, Minimum:

a.
Acrylic Emulsion:  10.0 percent.

b.
Hiding Pigment:  0.2 percent.

c.
Mineral Inert Fillers:  78.0 percent.

d.
Film Formers, Additives:  1.8 percent.

e.
Water:  8.5 percent.

4.
Weight per Gallon at 77 Degrees F:  15.2 lbs., plus or minus 1.0 lbs.

5.
Non-Volatile Material:  80 percent, plus or minus 5 percent.

Specifier Notes:  Specify color of crack filler.

6.
Color:  [Green]  [Neutral]  [Red].

D.
Patch Binder:  SportMaster “Acrylic Patch Binder”.

1.
100 percent acrylic emulsion liquid binder.

2.
Mix on-site with sand and cement.

3.
Levels and repairs low spots and depressions up to 3/4 inch deep in concrete pavement.

4.
Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

   E.
Adhesion Promoter:  SportMaster “Acrylic Adhesion Promoter”.

1.
Acrylic emulsion primer.

2.
Primes concrete surface and promotes adhesion of cushioned color coating system materials.

3.
Weight per Gallon at 77 Degrees F:  8.7 lbs., plus or minus 0.5 lbs.

F.
Filler Course:  SportMaster “Acrylic Resurfacer”.

1.
100 percent acrylic emulsion resurfacer.

2.
Mix on-site with silica sand.

3.
Apply to adhesion promoter or previously colored acrylic surfaces in preparation of cushioned color coating system.

4.
Chemical Characteristics, by Weight, Minimum:

a.
Acrylic Emulsion:  44.0 percent.

b.
Hiding Pigment:  2.0 percent.

c.
Mineral Inert Fillers:  5.0 percent.

d.
Film Formers, Additives:  0.2 percent.

e.
Water:  45.0 percent.

5.
Weight per Gallon at 77 Degrees F:  8.5 lbs., plus or minus 0.5 lbs.

6.
Non-Volatile Material:  27.5 percent, plus or minus 5.0 percent.

7.
Color:  Black or Neutral.
G.
Base Cushion:  CushionMaster II


1.      100 percent acrylic emulsion coating.


2.      Mix on-site with water.


3.      Coating with coarse rubber particles for higher cushion build.


4.      Weight per gallon at 77 Degrees F: 9.59 lbs., plus or minus.5 lbs.


5.      Non-Volatile Material:  55.92 percent, plus or minus 5 percent.

   H.
Finish Cushion:  CushionMaster I


1.      100 percent acrylic emulsion coating


2.      Mix on-site with water.


3.      Coating with fine rubber particles for smooth texturing.


4.      Weight per gallon at 77 Degrees F: 9.59 lbs., plus or minus.5 lbs.


5.      Non-Volatile Material:  55.92 percent, plus or minus 5 percent.

I.
Color Coating:  SportMaster “ColorPlus System”.

1.
100 percent acrylic emulsion coating.

2.
Mix on-site with silica sand and water.

3.
Color coats tennis courts.

4.
Weight per Gallon at 77 Degrees F:  9.2 lbs., plus or minus 0.5 lbs.

Specifier Notes:  Specify color of color coating.  The following colors can contribute to LEED credits for SS Credit 7.1: Heat Island Effect – Non-Roof:  Dove Gray, Ice Blue, Light Green, Red, and Sandstone.

5.
Color:  [Beige]  [Blue]  [Brown]  [Dark Green]  [Dove Gray]  [Forest Green]  [Gray]  [Ice Blue]  [Light Blue]  [Light Green]  [Maroon]  [Red]  [Sandstone]  [Tournament Purple].

J.
Line Markings Primer:  SportMaster “Stripe-Rite”.

1.
100 percent acrylic emulsion primer, clear drying.

2.
Primes line markings and prevents bleed-under for sharp lines.

3.
Chemical Characteristics, by Weight, Nominal:

a.
Acrylic Emulsion:  38.0 percent.

b.
Hiding Pigment:  0.0 percent.

c.
Mineral Inert Fillers:  7.0 percent.

d.
Film Formers, Additives:  1.5 percent.

e.
Water:  50.0 percent.

4.
Weight per Gallon at 77 Degrees F:  8.9 lbs., plus or minus 0.5 lbs.

5.
Non-Volatile Material:  29 percent, plus or minus 5 percent.

K.
Line Paint:  SportMaster “Textured Line Paint”.

1.
Pigmented, 100 percent acrylic emulsion line paint.

2.
Line marking on concrete tennis courts.

3.
Chemical Characteristics, by Weight, Nominal:

a.
Acrylic Emulsion:  25.89 percent.

b.
Pigment:  14.90 percent.

c.
Mineral Inert Fillers:  13.12 percent.

d.
Additives:  4.73 percent.

e.
Water:  41.36 percent.

4.
Weight per Gallon at 77 Degrees F:  10.65 lbs., plus or minus 0.75 lbs.

5.
Non-Volatile Material:  45.17 percent, plus or minus 5 percent.

Specifier Notes:  Specify color of line paint.

6.
Color:  [Blue]  [Red]  [White]  [Yellow].

PART 3
EXECUTION

3.1
EXAMINATION

A.
Examine concrete tennis court surfaces to receive cushioned color coating system.

B.
Verify:

1.
Suitable vapor barrier beneath concrete slab.

2.
Perimeter drainage to prevent moisture accumulation beneath concrete surface.

3.
Concrete tennis courts meet ASBA requirements.

C.
Notify Architect of conditions that would adversely affect application or subsequent use.

D.
Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2
SURFACE PREPARATION

A.
Protection of In-Place Conditions:  Protect adjacent surfaces and landscaping from contact with concrete tennis court surface color coating system.

B.
Prepare surfaces in accordance with manufacturer’s instructions.

C.
New Concrete:

1.
Cure new concrete surfaces a minimum of 28 days before application of concrete tennis court cushioned surface color coating system.

2.
Provide medium broom finish or similar roughened texture.

3.
Do not steel trowel finish.


4.      Acid etch surface per manufacturers specifications, then rinse thoroughly.
D.
Existing Concrete:

1.
Sandblast, shotblast, or scarify smooth concrete surfaces to roughened texture similar to medium broom finish.

2.
Acid etch surface per manufacturers specifications, then rinse thoroughly.
E.
Remove dirt, dust, debris, oil, grease, sealers, curing compounds, vegetation, loose coatings, loose materials, and other surface contaminants which could adversely affect application of concrete tennis court cushioned surface color coating system.  Pressure wash entire surface.
F.
Repair cracks, depressions, and surface defects in accordance with manufacturer’s instructions before application of color coating.

G.
Repair spalled areas and level depressions 1/8 inch and deeper with patch binder in accordance with manufacturer’s instructions.

H.
Apply adhesion promoter over entire concrete surface in accordance with manufacturer’s instructions.

I.
Apply 1 coat of filler course to provide smooth underlayment for application of cushioned color coating system.

J.
Ensure surface repairs are flush and smooth to adjoining surfaces.

3.3
APPLICATION

A.
Apply concrete tennis court cushioned surface color coating system in accordance with manufacturer’s instructions at locations indicated on the Drawings.

B.
Mix materials in accordance with manufacturer’s instructions.

C.
Apply Filler Course, Cushion Layers, and Color Coating with a 50-60 durometer, soft rubber squeegee.

D.
Filler Course:  Apply 1 coat on new concrete or existing acrylic surfaces.
E.     
Cushion Layers:  Apply 3 coats of the base layer (coarse granule) cushion, followed by 2 coats of the finish layer (fine granule) cushion in accordance with the manufacturer’s instructions.

F.
Color Coating:  Apply a minimum of 2 coats of color coating to prepared surfaces in accordance with manufacturer’s instructions.

G.
Allow material drying times in accordance with manufacturer’s instructions before applying other materials or opening completed surface to foot traffic.

3.4
LINE MARKINGS

A.
Lay out tennis court line markings in accordance with USTA Rules of Tennis.

B.
Apply line markings primer, after masking tape has been laid, to seal voids between masking tape and tennis court surface to prevent bleed-under when line paint is applied.

C.
Apply a minimum of 1 coat of line paint in accordance with manufacturer’s instructions.

3.5
PROTECTION

A.
Allow a minimum of 24 hours curing time before opening tennis courts for play.

B.
Protect applied concrete tennis court cushioned surface color coating system to ensure that, except for normal weathering, coating system will be without damage or deterioration at time of Substantial Completion.

END OF SECTION

SportMaster Concrete Tennis Court

Cushioned Surface Color Coating System
02790 (32 18 23.53) - 4

