SportMaster Sport Surfaces	April 2020

PO Box 2277

2520 South Campbell Street

Sandusky, Ohio 44870

Toll Free	800-326-1994

Fax	877-825-9226

Website	www.sportmaster.net

E-mail	moreinfo@sportmaster.net

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice, Fifth Edition.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers are from MasterFormat 1995 Edition, with section numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION 02790 (32 18 23.39)

CONCRETE RUBBERIZED RUNNING TRACK SURFACE COATING SYSTEM

Specifier Notes:  This section covers SportMaster Sport Surfaces “SportMaster” concrete rubberized running track surface coating system.  Consult SportMaster Sport Surfaces for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Concrete rubberized running track surface coating system.

1.2	RELATED REQUIREMENTS

Specifier Notes:  Edit the following list of related sections as required.  Delete related sections not required.  List other sections with work directly related to this section.

A.	Section 02975 (32 01 17.63) – Rubberized Running Track Surface Crack Repair System:  Repairing cracks in concrete tracks.

1.3	REFERENCE STANDARDS

Specifier Notes:  List reference standards mentioned in this section, complete with designations and titles.  Delete reference standards not included in this edited section.  This article does not require compliance with reference standards, but is merely a listing of those used.

A.	American Sports Builders Association (ASBA)

B.	International Association of Athletic Federations (IAAF)

C.	National Association of Intercollegiate Athletics (NAIA)

D.	National Federation of State High School Associations (NFHS) Rule Book

E.	National Collegiate Athletic Association (NCAA) Rule Book

F.      USA Track & Field (USATF)

1.4	SUBMITTALS

A.	Comply with Section 01330 (01 33 00) – Submittal Procedures.

B.	Product Data:  Submit manufacturer’s product data, including surface and crack preparation and application instructions.

C.	Samples:  Submit manufacturer’s color samples of color coating.

D.	Test Reports:

- Submit independent test results for solar reflectance index.

- Submit independent test results for 2000 Hour ASTM G154, accelerated weathering UV test, to demonstrate long-term durability and fade resistance.

- Submit independent test results for 2000 Hour, accelerated weathering ASTM G155 Xenon Arc test, to demonstrate long-term fade resistance and quality of pigment.

E.	Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

F.	Manufacturer’s Project References:  Submit manufacturer’s list of successfully completed concrete rubberized running track surface coating system projects, including project name, location, and date of application.

G.	Applicator’s Project References:  Submit applicator’s list of successfully completed concrete rubberized running track surface coating system projects, including project name, location, type and quantity of color coating system applied, and date of application.

H.	Warranty Documentation:  Submit manufacturer’s standard warranty.

- Authorized Installer Certificate:  Submit manufacturer’s authorized installer certificate.

1.5	QUALITY ASSURANCE

A.	Manufacturer’s Qualifications:

1.	Manufacturer regularly engaged, for past 5 years, in manufacture of concrete rubberized running track surface coating systems of similar type to that specified.

2.	United States owned company.

3.	Member:  ASBA.

B.	Applicator's Qualifications:

1.	Applicator regularly engaged, for past 3 years, in application of rubberized running track surface coating systems of similar type to that specified.

2.	Employ persons trained for application of rubberized running track surface coating systems.

3.	Applicator must be authorized installer of the surfacing brand used.

1.6	DELIVERY, STORAGE, AND HANDLING

A.	Delivery and Acceptance Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.	Storage and Handling Requirements:

1.	Store and handle materials in accordance with manufacturer’s instructions.

2.	Keep materials in manufacturer’s original, unopened containers and packaging until application.

3.	Store materials in clean, dry area indoors.

4.	Store materials out of direct sunlight.

5.	Keep materials from freezing.

6.	Protect materials during storage, handling, and application to prevent contamination or damage.

7.	Close containers when not in use.

8.	Retain manufacturer batch codes on each container and application dates, for warranty purposes.

1.7	AMBIENT CONDITIONS

A.	Do not apply concrete rubberized running track surface coating system when air or surface temperatures are below 50°F (10°C) during application or within 24 hours after application.

B.	Do not apply concrete rubberized running track surface coating system when rain is expected during application or within 24 hours after application.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	SportMaster Sport Surfaces, PO Box 2277, 2520 South Campbell Street, Sandusky, Ohio 44870.  Toll Free 800-326-1994.  Fax 877-825-9226.  Website www.sportmaster.net.  E-mail moreinfo@sportmaster.net.

All other brands must be pre-approved by the architect/owner, 7 days prior to the bid date.  If submitting another brand, bidder must furnish copies of all submittal documents under section 1.4

2.2	MATERIALS

A.	Concrete Rubberized Running Track Surface Coating System:  TrackMaster Plus Coating System.

B.	Crack Sealant:  SportMaster “TrackFlex or CourtFlex”.

1.	100 percent acrylic emulsion elastomeric crack sealant.

2.	Seals cracks up to 1/2 inch wide in concrete pavement & track surfaces.

3.	Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

4.	Non-Volatile Material:  61 percent, plus or minus 5 percent.

5.	Color:  [Black] [Red] [Green] [Neutral]

C.	Patching Compound (Rubberized):  SportMaster “Lane One”.

1.	100 percent acrylic emulsion trowel-grade leveling, patching and crack repair product.

2.	Fills cracks in concrete pavement up to 1 inch wide.

3.      Levels depressions in rubberized track surfaces.

4.	Weight per Gallon at 77 Degrees F:  9.86 pounds., plus or minus 0.5 lbs.

5.	Non-Volatile Material:  54.442%, plus or minus 5 percent.

6.	Color:  Black

D.	Patch Binder:  SportMaster “Acrylic Patch Binder”.

1.	100 percent acrylic emulsion liquid binder.

2.	Mix on-site with sand and cement.

3.	Levels and repairs low spots and depressions up to 3/4 inch deep in concrete pavement.

4.	Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

E.	Adhesion Promoter:  SportMaster “Acrylic Adhesion Promoter”.

1.	Acrylic emulsion primer.

2.	Primes concrete surface and promotes adhesion of color coating system materials.

3.	Weight per Gallon at 77 Degrees F:  8.7 lbs., plus or minus 0.5 lbs.

F.	Filler Course:  SportMaster “Acrylic Resurfacer”.

1.	100 percent acrylic emulsion resurfacer.

2.	Mix on-site with silica sand.

3.	Apply to new concrete surfaces or previously colored, smooth acrylic surfaces in preparation of rubberized running track surface coating system.

4.	Chemical Characteristics, by Weight, Minimum:

a.	Acrylic Emulsion:  44.0 percent.

b.	Hiding Pigment:  2.0 percent.

c.	Mineral Inert Fillers:  5.0 percent.

d.	Film Formers, Additives:  0.2 percent.

e.	Water:  45.0 percent.

5.	Weight per Gallon at 77 Degrees F:  8.5 lbs., plus or minus 0.5 lbs.

6.	Non-Volatile Material:  27.5 percent, plus or minus 5.0 percent.

7.	Color:  [Black]  [Neutral].

G.	Track Surface:  SportMaster “TrackMaster Plus”.

1.	100 percent acrylic emulsion coating.

2.	Mix on-site with water.

3.	Color coats concrete or existing latex running tracks.

4.	Weight per Gallon at 77 Degrees F:  9.3 lbs., plus or minus 0.5 lbs.

Specifier Notes:  Specify color of color coating.  The following colors can contribute to LEED credits for SS Credit 7.1: Heat Island Effect – Non-Roof:  Dove Gray, Ice Blue, Light Green, Red, Sandstone, Orange & Yellow. Also note * are premium cost colors.

5.	Color:  [Beige]  [Blue]  [Brown]  [Dark Green]  [Dove Gray]  [Forest Green]  [Gray]  [Ice Blue]  [Light Blue]  [Light Green]  [Maroon]  [Red]  [Sandstone]  [Tournament Purple*]  [Orange*]  [Yellow] [Brite Red*] [Black]

H.	Line Paint:  SportMaster “Liquid Thermoplastic” Line Paint.

1.	Pigmented, 100 percent acrylic emulsion line paint.

2.	Line marking on concrete running track surfaces.

3.	Solids (by weight %): 77.5

4.	Weight per Gallon at 77 Degrees F:  14.1 lbs.

Specifier Notes:  Specify color of line paint.

5.	Color:  [Blue]  [Red]  [White]  [Yellow].

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine concrete running track surface to receive rubberized running track surface coating system.

B.	Verify:

1.	Suitable vapor barrier beneath concrete slab.

2.	Perimeter drainage to prevent moisture accumulation beneath concrete surface.

3.	Curing compounds have not been used on concrete surface.

4.	Concrete surface has a medium-broom texture for good physical adhesion of coatings.

5.	Concrete running track surface meets all ASBA construction requirements.

C.	Notify Architect of conditions that would adversely affect application or subsequent use.

D.	Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2	SURFACE PREPARATION

A.	Protection of In-Place Conditions:  Protect adjacent surfaces and landscaping from contact with concrete rubberized running track surface coating system.

B.	Prepare surfaces in accordance with manufacturer’s instructions.

C.	New Concrete:

1.	Cure new concrete surfaces a minimum of 28 days before application of rubberized running track coating system.

2.	Provide medium broom finish or similar roughened texture.

3.	Do not steel trowel finish.

4.      Acid etch with phosphoric or muriatic acid and rinse thoroughly prior to application of color

coating system.

D.	Existing Concrete:

1.	Sandblast, shotblast, or scarify smooth concrete surfaces to roughened texture similar to medium broom finish.  If shot blasting, a shot blast profile of CSP3 or CSP4 is recommended.

2.	If existing concrete is uncoated, acid etch with phosphoric or muriatic acid and rinse thoroughly prior to application of color coating system

.

E.	Remove dirt, dust, debris, oil, grease, vegetation, loose materials, and other surface contaminants which could adversely affect application of concrete rubberized running track surface coating system.  Pressure wash entire surface.

F.	Repair cracks, depressions, and surface defects in accordance with manufacturer’s instructions before application of filler course and track surface.

G.	Level concrete depressions 1/8 inch and deeper with patch binder in accordance with manufacturer’s instructions.

H.     Level depressions in existing rubberized latex track surfaces 1/8 inch and deeper with

rubberized patching compound in accordance with manufacturer’s instructions.

I.	Apply 1 coat of adhesion promoter as required by manufacturer for good adhesion of the running track coating system to the concrete surface.

J.	Apply 1 or 2 coats of filler course as required by surface roughness and porosity to provide smooth underlayment for application of track surface.

K.	Ensure surface repairs are flush and smooth to adjoining surfaces.

3.3	APPLICATION

A.	Apply concrete rubberized running track surface coating system in accordance with manufacturer’s instructions at locations indicated on the Drawings.

B.	Mix materials in accordance with manufacturer’s instructions.

C.	Filler Course:

1.	Apply 2 coats on new concrete or existing acrylic surfaces with extensive cracks or low spot repair.

2.	Apply 1 coat on existing acrylic surfaces with minimal repairs or a smooth finish that requires texture for proper application of rubberized running track surface coatings.

3.      Filler Course not recommended on existing SBR latex tracks.

Specifier Notes:  Specify number of track surface coats.  Minimum of 2 coats required.  Additional coats add to the thickness and shock absorption of the surface.

D.	Track Surface:  Apply a minimum of [2] coats of color coating to prepared surfaces in accordance with manufacturer’s instructions, on the product data sheet.

E.	Allow material drying times in accordance with manufacturer’s instructions before applying other materials or opening completed surface to foot traffic.

3.4	LINE MARKINGS

- Lay out running track line markings in accordance with appropriate governing body:

  - International Association of Athletic Federations (IAAF)

  - National Association of Intercollegiate Athletics (NAIA)

  - National Federation of State High School Associations (NFHS)

  - National Collegiate Athletic Association (NCAA) Rule Book

  - USA Track & Field (USATF)

B.	Apply a minimum of 1 coat of line paint in accordance with manufacturer’s instructions.

3.5	PROTECTION

A.	Allow a minimum of 48 hours curing time before opening concrete rubberized running track for play.

B.	Protect applied concrete rubberized running track surface coating system to ensure that, except for normal weathering, coating system will be without damage or deterioration at time of Substantial Completion.

END OF SECTION