SportMaster Sport Surfaces (Division of SealMaster)	April 2025

PO Box 2277

2520 South Campbell Street

Sandusky, Ohio 44870

Toll Free	800-326-1994

Fax	877-825-9226

Website	www.sportmaster.net

E-mail	moreinfo@sportmaster.net

Product Guide Specification

Specifier Notes:  This product guide specification is written according to the Construction Specifications Institute (CSI) 3-Part Format, including MasterFormat, SectionFormat, and PageFormat, as described in The Project Resource Manual—CSI Manual of Practice, Fifth Edition.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code.  Coordinate this section with other specification sections and the Drawings.  Delete all “Specifier Notes” after editing this section.

Section numbers are from MasterFormat 1995 Edition, with section numbers from MasterFormat 2004 Edition in parentheses.  Delete version not required.

SECTION 02790 (32 18 00)

ASPHALT TRAFFIC GARDEN SURFACE COLOR COATING SYSTEM

Specifier Notes:  This section covers SportMaster Sport Surfaces “SportMaster” asphalt traffic garden surface color coating system.  Consult SportMaster Sport Surfaces for assistance in editing this section for the specific application.

PART 1	GENERAL

1.1	SECTION INCLUDES

A.	Asphalt traffic garden surface color coating system.

1.2	RELATED REQUIREMENTS

Specifier Notes:  Edit the following list of related sections as required.  Delete related sections not required.  List other sections with work directly related to this section.

A.	Section 02975 (32 01 17.63) – Traffic garden Crack Repair System:  Repairing cracks in asphalt traffic garden surfaces with 3rd party, multi-layer fabric systems.

1.3	REFERENCE STANDARDS

Specifier Notes:  List reference standards mentioned in this section, complete with designations and titles.  Delete reference standards not included in this edited section.  This article does not require compliance with reference standards, but is merely a listing of those used.

A.	American Sports Builders Association (ASBA).

1.4	SUBMITTALS

A.	Comply with Section 01330 (01 33 00) – Submittal Procedures.

B.	Product Data:  Submit manufacturer’s product data, including surface and crack preparation and application instructions.

C.	Samples:  Submit manufacturer’s color samples of color coating.

D.	Test Reports:

- Submit independent test results for solar reflectance index.

- Submit independent test results for 2000 Hour ASTM G154, accelerated weathering UV test, to demonstrate long-term durability and fade resistance.

- Submit independent test results for 2000 Hour, accelerated weathering ASTM G155 Xenon Arc test, to demonstrate long-term fade resistance and quality of pigment.

E.	Manufacturer’s Certification:  Submit manufacturer’s certification that materials comply with specified requirements and are suitable for intended application.

F.	Manufacturer’s Project References:  Submit manufacturer’s list of successfully completed asphalt traffic garden surface color coating system projects, including project name, location, and date of application.

G.	Applicator’s Project References:  Submit applicator’s list of successfully completed asphalt traffic garden surface color coating system projects, including project name, location, type and quantity of color coating system applied, and date of application.

H.	Warranty Documentation:  Submit manufacturer’s standard warranty.

I.	Authorized Installer Certificate:  Submit manufacturer’s authorized installer certificate.

1.5	QUALITY ASSURANCE

A.	Manufacturer’s Qualifications:

1.	Manufacturer regularly engaged, for past 5 years, in manufacture of asphalt traffic garden surface color coating systems of similar type to that specified.

2.	United States owned company.

3.	Member:  ASBA.

B.	Applicator's Qualifications:

1.	Applicator regularly engaged, for past 3 years, in application of traffic garden surface color coating systems of similar type to that specified.

2.	Employ persons trained for application of traffic garden surface color coating systems.

3.	Applicator must be authorized installer of the surfacing brand used.

1.6	DELIVERY, STORAGE, AND HANDLING

A.	Delivery and Acceptance Requirements:  Deliver materials to site in manufacturer’s original, unopened containers and packaging, with labels clearly identifying product name and manufacturer.

B.	Storage and Handling Requirements:

1.	Store and handle materials in accordance with manufacturer’s instructions.

2.	Keep materials in manufacturer’s original, unopened containers and packaging until application.

3.	Store materials in clean, dry area indoors.

4.	Store materials out of direct sunlight.

5.	Keep materials from freezing.

6.	Protect materials during storage, handling, and application to prevent contamination or damage.

7.	Close containers when not in use.

8.	Retain manufacturer batch codes on each container and application dates, for warranty purposes.

1.7	AMBIENT CONDITIONS

A.	Do not apply asphalt traffic garden surface color coating system when air or surface temperatures are below 50°F (10°C) during application or within 24 hours after application.

B.	Do not apply asphalt traffic garden surface color coating system when rain is expected during application or within 24 hours after application.

PART 2	PRODUCTS

2.1	MANUFACTURER

A.	SportMaster Sport Surfaces, PO Box 2277, 2520 South Campbell Street, Sandusky, Ohio 44870.  Toll Free 800-326-1994.  Fax 877-825-9226.  Website www.sealmaster.net.  E-mail info@sealmaster.net.

All other brands must be pre-approved by the architect/owner, 7 days prior to the bid date.  If submitting another brand, bidder must furnish copies of all submittal documents under section 1.4

2.2	MATERIALS

A.	Asphalt Traffic Garden Surface Color Coating System:  The ColorPave System by SealMaster

B.	Crack Sealant:  SportMaster “Crack Magic”.

1.	100 percent acrylic emulsion elastomeric crack sealant.

2.	Seals cracks up to 1/2 inch wide in asphalt pavement.

3.	Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

4.	Non-Volatile Material:  61 percent, plus or minus 5 percent.

C.	Crack Filler:  SportMaster “Acrylic Crack Patch”.

1.	100 percent acrylic emulsion trowel-grade crack filler.

2.	Fills cracks in asphalt pavement up to 1 inch wide.

3.	Chemical Characteristics, by Weight, Minimum:

a.	Acrylic Emulsion:  10.0 percent.

b.	Hiding Pigment:  0.2 percent.

c.	Mineral Inert Fillers:  78.0 percent.

d.	Film Formers, Additives:  1.8 percent.

e.	Water:  8.5 percent.

4.	Weight per Gallon at 77 Degrees F:  15.2 lbs., plus or minus 1.0 lbs.

5.	Non-Volatile Material:  80 percent, plus or minus 5 percent.

6.	Color:  [Green] [Neutral] [Red] [Blue].

D.	Patch Binder:  SportMaster “Acrylic Patch Binder”.

1.	100 percent acrylic emulsion liquid binder.

2.	Mix on-site with sand and cement.

3.	Levels and repairs low spots and depressions up to 3/4 inch deep in asphalt pavement.

4.	Weight per Gallon at 77 Degrees F:  8.8 lbs., plus or minus 0.5 lbs.

E.	Filler Course:  SealMaster “ColorPave”.

1.	100 percent acrylic emulsion resurfacer.

2.	Mix on-site with silica sand, up to 15 lbs of 50-60 mesh silica sand, per gallon.

3.	Apply to asphalt surfaces or previously colored acrylic surfaces in preparation of color coating system.

4.	Chemical Characteristics, by Weight, Minimum:

a.	Acrylic Emulsion:  44.0 percent.

b.	Hiding Pigment:  2.0 percent.

c.	Mineral Inert Fillers:  5.0 percent.

d.	Film Formers, Additives:  0.2 percent.

e.	Water:  45.0 percent.

5.	Weight per Gallon at 77 Degrees F:  8.5 lbs., plus or minus 0.5 lbs.

6.	Non-Volatile Material:  27.5 percent, plus or minus 5.0 percent.

7.	Color:  [Neutral or Pigmented with ColorPlus Pigment Dispersion].

F.	Color Coating:  SealMaster “ColorPave”.

1.	100 percent acrylic emulsion coating.

2.	Mix on-site with silica sand and water (ColorPave Neutral Concentrate & ColorPlus Pigment Dispersion

3.	Color coats traffic garden surfaces & game courts.

4.	Weight per Gallon at 77 Degrees F:  9.2 lbs., plus or minus 0.5 lbs.

Specifier Notes:  Specify color of color coating.  The following colors can contribute to LEED credits for SS Credit 7.1: Heat Island Effect – Non-Roof:  Dove Gray, Ice Blue, Light Green, Red, Sandstone, Orange, Brite Red* & Yellow. Also note * are premium cost colors.

5.	Color:  [Beige]  [Blue]  [Brown]  [Dark Green]  [Dove Gray]  [Forest Green]  [Gray]  [Ice Blue]  [Light Blue]  [Light Green]  [Maroon]  [Red]  [Sandstone]  [*Tournament Purple]  [*Orange]  [Yellow] [*Brite Red] [Black] – ColorPlus Fusion System is also available with hundreds of color options: https://www.sportmaster.net/colorplusfusion/

G.	Line Markings Primer:  SportMaster “Stripe-Rite”.

1.	100 percent acrylic emulsion primer, clear drying.

2.	Primes line markings and prevents bleed-under for sharp lines.

3.	Chemical Characteristics, by Weight, Nominal:

a.	Acrylic Emulsion:  38.0 percent.

b.	Hiding Pigment:  0.0 percent.

c.	Mineral Inert Fillers:  7.0 percent.

d.	Film Formers, Additives:  1.5 percent.

e.	Water:  50.0 percent.

4.	Weight per Gallon at 77 Degrees F:  8.9 lbs., plus or minus 0.5 lbs.

5.	Non-Volatile Material:  29 percent, plus or minus 5 percent.

H.	Line Paint:  SportMaster “Textured Line Paint”.

1.	Pigmented, 100 percent acrylic emulsion line paint.

2.	Line marking on asphalt traffic gardens.

3.	Chemical Characteristics, by Weight, Nominal:

a.	Acrylic Emulsion:  25.89 percent.

b.	Pigment:  14.90 percent.

c.	Mineral Inert Fillers:  13.12 percent.

d.	Additives:  4.73 percent.

e.	Water:  41.36 percent.

4.	Weight per Gallon at 77 Degrees F:  10.65 lbs., plus or minus 0.75 lbs.

5.	Non-Volatile Material:  45.17 percent, plus or minus 5 percent.

6.	Color:  White.

PART 3	EXECUTION

3.1	EXAMINATION

A.	Examine asphalt traffic garden surfaces to receive color coating system.

B.	Verify asphalt traffic gardens meet ASBA requirements.

C.	Notify Architect of conditions that would adversely affect application or subsequent use.

D.	Do not begin surface preparation or application until unacceptable conditions are corrected.

3.2	SURFACE PREPARATION

A.	Protection of In-Place Conditions:  Protect adjacent surfaces and landscaping from contact with asphalt traffic garden surface color coating system.

B.	Prepare surfaces in accordance with manufacturer’s instructions.

C.	Cure new asphalt surfaces a minimum of 14 to 30 days before application of asphalt traffic garden surface color coating system.

D.	Remove dirt, dust, debris, oil, grease, vegetation, loose materials, and other surface contaminants which could adversely affect application of asphalt traffic garden surface color coating system.  Pressure wash entire surface.

E.	Repair cracks, depressions, and surface defects in accordance with manufacturer’s instructions before application of filler course and color coating.

F.	Level depressions 1/8 inch and deeper with patch binder in accordance with manufacturer’s instructions.

G.	Apply 1 or 2 coats of filler course as required by surface roughness and porosity to provide smooth underlayment for application of color coating.

H.	Ensure surface repairs are flush and smooth to adjoining surfaces.

3.3	APPLICATION

A.	Apply asphalt traffic garden surface color coating system in accordance with manufacturer’s instructions at locations indicated on the Drawings.

B.	Mix materials in accordance with manufacturer’s instructions.

C.	Apply Filler Course and Color Coating with a 50-60 durometer, soft rubber squeegee.

D.	Filler Course:

1.	Apply 2 coats on new asphalt or existing acrylic surfaces with extensive cracks or low spot repair.

2.	Apply 1 coat on existing acrylic surfaces with minimal repairs.

E.	Color Coating:  Apply a minimum of 2 coats of color coating to prepared surfaces in accordance with manufacturer’s instructions.

F.	Allow material drying times in accordance with manufacturer’s instructions before applying other materials or opening completed surface to foot traffic.

3.4	LINE MARKINGS

- Lay out traffic garden design, games and marking per architect drawings.

B.	Apply line markings primer, after masking tape has been laid, to seal voids between masking tape and traffic garden surface to prevent bleed-under when line paint is applied.

C.	Apply a minimum of 1 coat of line paint in accordance with manufacturer’s instructions.

3.5	PROTECTION

A.	Allow a minimum of 48 hours curing time before opening traffic garden for play.

B.	Protect applied asphalt traffic garden surface color coating system to ensure that, except for normal weathering, coating system will be without damage or deterioration at time of Substantial Completion.

END OF SECTION